1.	GENERAL REQUIREMENTS

1.1	Scope

The following describes parameters for the manufacture, supply, and installation of Poly-Flex® polyethylene geomembranes. All procedures, operations, and methods shall be in accordance with the engineer’s specifications, plans, and drawings.

1.2	Qualifications

1.2.1	Manufacturing

The manufacturer shall have at least five (5) years continuous experience in manufacturing polyethylene geomembrane and/or experience totaling 10,000,000 square feet of manufactured polyethylene geomembrane.

1.2.2	Installation

The installation contractor shall be a dealer trained to install geomembrane.

Installation shall be performed under the constant direction of a field installation supervisor who shall remain on site and be responsible, throughout the liner installation, for liner layout, seaming, testing, repairs, and all other activities by the Installer. The field installation supervisor shall have installed or supervised the installation of a minimum of 2,000,000 square feet of polyethylene geomembrane. Seaming shall be performed under the direction of a master seamer (who may also be the field installation supervisor) who has seamed a minimum of 2,000,000 square feet of polyethylene geomembrane, using the same type of seaming apparatus specified for this project. The field installation supervisor and/or master seamer shall be present whenever seaming is performed.

1.3	Submittals

1.3.1	Manufacturer

The manufacturer shall provide the following information:

A.	Submittals with Bid Documents

1.	List of material properties.

2.	Manufacturing quality control program.

B.	Submittals After Contract Award, Prior to Liner Installation

1.	Copy of quality control certificates issued by the resin supplier.

2.	Copy of quality control certificates for the geomembranes in conformance with Section 2.4.3.

1.3.2	Installation Contractor

The installer shall provide the following written information:

A.	Submittals With Bid Documents

A list of completed facilities, totaling a minimum of 2,000,000 square feet, for which the installer has installed polyethylene geomembrane. For each installation, the following information shall be provided:

a. Name and purpose of facility, location, and date of installation.

b. Name of owner, design engineer, manufacturer, and name and telephone number of contact at the facility who can discuss the project.

c.	Thickness and quantity of the installed geomembrane.

B.	Submittals by Successful Bidder Prior to Commencement of Installation

1.	Proposed installation panel layout.

2.	Resume(s) of the field installation supervisor and master seamer.

1.4	Meeting

A daily meeting shall be held at the work area just prior to commencement of the work to discuss work activities. The earthwork contractor, the liner installer, and the inspector shall be present.

1.5	Warranty

A written Warranty shall be obtained from the manufacturer (for material) and the installation contractor (for workmanship). These documents shall warrant both the quality of the material and workmanship for a specified duration of time.

2.	MATERIAL SPECIFICATIONS

2.1	Materials

1.	The geomembrane shall be High-Density Polyethylene (HDPE) or Linear Low Density Polyethylene (LLDPE).

2.	Gasket material shall be neoprene, closed cell medium, 1/4-inch thick, 2 inches wide with adhesive on one side, or other compatible gasket materials as required.

3.	Metal battens or banding and hardware shall be stainless steel.

4.	Sealant shall be General Electric Silicone, RTV 103, or equivalent.

2.2	Geomembrane Raw Materials

The geomembrane shall be manufactured of polyethylene resins produced in the United States and shall be compounded and manufactured specifically for the intended purpose. The resin manufacturer shall certify each lot for the following properties:

The natural polyethylene resin without the carbon black shall meet the following requirements:

Property	                                              Test Method		HDPE	LLDPE

Requirements	Requirements

Density, g/cc	ASTM D 4883, ASTM D 1505, or ASTM D 792	0.932 - 0.940	0.915 - 0.926

Melt Index, g/10 min.	ASTM D 1238 Condition E	<1.0	<1.0

2.3	Rolls

The geomembrane shall be a minimum 23 ft seamless width, as manufactured by Poly-America, L.P. (2000 W. Marshall Dr., Grand Prairie, TX 75051, 888-765-9359). Carbon black shall be added to the resin if the resin is not compounded for ultra-violet resistance.

The surface of the smooth geomembrane shall not have striations, roughness, pinholes, or bubbles.

The geomembrane shall be supplied in rolls. Labels on each roll shall identify the thickness of the material, the length and width of the roll, lot and roll numbers, and name of manufacturer.

Applicable Test Methods

ASTM International

ASTM D 792	Specific gravity (relative density) and density of plastics by displacement

ASTM D 1004	Initial tear resistance of plastic sheeting

ASTM D 1238	Flow rates of thermoplastics by extrusion plastometers

ASTM D 1505	Density of plastics by the density-gradient technique

ASTM D 1603	Carbon black in olefin plastics

ASTM D 1898	Sampling of plastics

ASTM D 3895	Oxidative induction time of polyolefins by thermal analysis

ASTM D 4833	Index Puncture Resistance of geotextiles, geomembranes and related products

ASTM D 4883	Density of polyethylene by the Ultrasound technique

ASTM D 5199	Measuring nominal thickness of geotextiles and geomembrane

ASTM D 5323	Determination of 2% secant modulus for polyethylene geomembranes

ASTM D 5397	Procedure to perform a single-point notched constant tensile load - Appendix (SP-NCTL) test

ASTM D 5596	Microscopic evaluation of the dispersion of carbon black in polyolefin geosynthetics

ASTM D 5617	Multi-axial tension test for geosynthetics

ASTM D 5641	Practice for geomembrane seam evaluation by vacuum chamber

ASTM D 5721	Practice for air-oven aging of polyolefin geomembranes

ASTM D 5820	Practice for the pressurized air channel evaluation of dual-seamed geomembrane

ASTM D 5885	Oxidative induction time of polyolefin geosynthetics by high pressure differential scanning calorimetry

ASTM D 5994	Measuring the core thickness of textured geomembranes

ASTM D 6392	Determining the integrity of nonreinforced geomembrane seams produced using thermo-fusing methods

ASTM D 6693	Determining tensile properties of nonreinforced polyethylene and nonreinforced flexible polypropylene geomembranes

ASTM D 7238	Effect of exposure of unreinforced polyolefin geomembrane using fluorescent UV condensation apparatus

ASTM D 7466	Measuring the asperity height of textured geomembrane

Geosynthetic Research Institute (GRI)

GRI GM 10	Specification for the stress crack resistance of geomembrane sheet

GRI GM 19	Seam strength and related properties of thermally bonded polyolefin geomembranes

The geomembrane rolls shall meet the following specifications:

SMOOTH HDPE GEOMEMBRANE (ENGLISH UNITS)

Minimum Average Values

Property				    Test Method		30 mil	  40 mil	    60 mil         80 mil      100 mil

Thickness, mils	ASTM D 5199

minimum average		30	40	60	80	100

lowest individual reading		27	36	54	72	90

Sheet Density, g/cc	 ASTM D 1505/D 792	0.940	0.940	0.940	0.940	0.940

Tensile Properties1	ASTM D 6693

1. Yield Strength, lb/in	 	63	84	126	168	210

2. Break Strength, lb/in	 	114	152	228	304	380

3. Yield Elongation, %		12	12	12	12	12

4. Break Elongation, %		700	700	700	700	700

Tear Resistance, lb	ASTM D 1004	21	28	42	56	70

Puncture Resistance, lb	ASTM D 4833	54	72	108	144	180

Stress Crack Resistance2, hrs	ASTM D 5397 (App.)	300	300	300	300	300

Carbon Black Content3, %	ASTM D 1603	2.0 - 3.0	2.0 - 3.0	2.0 - 3.0	2.0 - 3.0	2.0 - 3.0

Carbon Black Dispersion	ASTM D 5596			--Note 4--

Oxidative Induction Time (OIT)

Standard OIT, minutes	ASTM D 3895	100	100	100	100	100

Oven Aging at 85°C	ASTM D 5721

High Pressure OIT - % retained after 90 days	ASTM D 5885	80	80	80	80	80

UV Resistance5	ASTM D 7238

High Pressure OIT6 - % retained after 1600 hrs	 ASTM D 5885	50	50	50	50	50

Roll Dimensions

1. Width (feet):		23	23	23	23	23

2. Length (feet)		1000	750	500	375	300

3. Area (square feet):		23,000	17,250	11,500	8,625	6,900

4. Gross weight (pounds, approx.)		3,470	3,470	3,470	3,470	3,470

1	Machine direction (MD) and cross machine direction (XMD) average values should be on the basis of 5 test specimens each direction.

Yield elongation is calculated using a gauge length of 1.3 inches; Break elongation is calculated using a gauge length of 2.0 inches.

2	The yield stress used to calculate the applied load for the SP-NCTL test should be the mean value via MQC testing.

3	Other methods such as ASTM D 4218 or microwave methods are acceptable if an appropriate correlation can be established.

4	Carbon black dispersion for 10 different views: Nine in Categories 1 and 2 with one allowed in Category 3.

5	The condition of the test should be 20 hr. UV cycle at 75°C followed by 4 hr. condensation at 60°C.

6	UV resistance is based on percent retained value regardless of the original HP-OIT value.

SMOOTH HDPE GEOMEMBRANE (METRIC UNITS)

Minimum Average Values

Property	Test Method	0.75 mm	1.00 mm	1.50 mm	2.00 mm	2.50 mm

Thickness, microns	ASTM D 5199

minimum average		750	1,000	1,500	2,000	2,500

lowest individual reading		675	900	1,350	1,800	2,250

Sheet Density, g/cc	 ASTM D 1505/D 792	0.940	0.940	0.940	0.940	0.940

Tensile Properties1	ASTM D 6693

1. Yield Strength, kN/m	 	11	15	22	29	37

2. Break Strength, kN/m	 	20	27	40	53	67

3. Yield Elongation, %		12	12	12	12	12

4. Break Elongation, %		700	700	700	700	700

Tear Resistance, N	ASTM D 1004	93	125	187	249	311

Puncture Resistance, N	ASTM D 4833	240	320	480	640	800

Stress Crack Resistance2, hrs	ASTM D 5397 (App.)	300	300	300	300	300

Carbon Black Content3, %	ASTM D 1603	2.0 - 3.0	2.0 - 3.0	2.0 - 3.0	2.0 - 3.0	2.0 - 3.0

Carbon Black Dispersion	ASTM D 5596			--Note 4--

Oxidative Induction Time (OIT)

Standard OIT, minutes 	ASTM D 3895	100	100	100	100	100

Oven Aging at 85°C	ASTM D 5721

High Pressure OIT - % retained after 90 days	ASTM D 5885	80	80	80	80	80

UV Resistance5	ASTM D 7238

High Pressure OIT6 - % retained after 1600 hrs	ASTM D 5885	50	50	50	50	50

Roll Dimensions

1. Width (meters):		7	7	7	7	7

2. Length (meters)		304.9	228.7	152.4	114.3	91.5

3. Area (square meters):		2,137	1,603	1,068	801	641

4. Gross weight (kilograms, approx.)		1,574	1,574	1,574	1,574	1,574

1	Machine direction (MD) and cross machine direction (XMD) average values should be on the basis of 5 test specimens each direction.

Yield elongation is calculated using a gauge length of 33 mm; Break elongation is calculated using a gauge length of 50 mm.

2	The yield stress used to calculate the applied load for the SP-NCTL test should be the mean value via MQC testing.

3	Other methods such as ASTM D 4218 or microwave methods are acceptable if an appropriate correlation can be established.

4	Carbon black dispersion for 10 different views: Nine in Categories 1 and 2 with one allowed in Category 3.

5	The condition of the test should be 20 hr. UV cycle at 75°C followed by 4 hr. condensation at 60°C.

6	UV resistance is based on percent retained value regardless of the original HP-OIT value.

TEXTURED HDPE GEOMEMBRANE (ENGLISH UNITS)

Minimum Average Values

Property	Test Method	40 mil	60 mil	80 mil	100 mil

Thickness, mils	ASTM D 5994

minimum average		38	57	76	95

lowest individual of 8 of 10 readings		36	54	72	90

lowest individual of 10 readings		34	51	68	85

Asperity Height1, mils	ASTM D 7466	10	10	10	10

Sheet Density, g/cc	 ASTM D 1505/D 792	0.940	0.940	0.940	0.940

Tensile Properties2	ASTM D 6693

1. Yield Strength, lb/in	 	84	126	168	210

2. Break Strength, lb/in	 	60	90	120	150

3. Yield Elongation, %		12	12	12	12

4. Break Elongation, %		100	100	100	100

Tear Resistance, lb	ASTM D 1004	28	42	56	70

Puncture Resistance, lb	ASTM D 4833	60	90	120	150

Stress Crack Resistance3, hrs	ASTM D 5397 (App.)	300	300	300	300

Carbon Black Content4, %	ASTM D 1603	2.0 - 3.0	2.0 - 3.0	2.0 - 3.0	2.0 - 3.0

Carbon Black Dispersion	ASTM D 5596		                 --Note 5--

Oxidative Induction Time (OIT)

Standard OIT, minutes	ASTM D 3895	100	100	100	100

Oven Aging at 85°C	ASTM D 5721

High Pressure OIT - % retained after 90 days	ASTM D 5885		80	80	80	80

UV Resistance6	ASTM D 7238

High Pressure OIT7 - % retained after 1600 hrs	ASTM D 5885	50	50	50	50

Roll Dimensions

1. Width (feet):		23	23	23	23

2. Length (feet)		750	500	375	300

3. Area (square feet):		17,250	11,500	8,625	6,900

4. Gross weight (pounds, approx.)		3,500	3,500	3,470	3,470

1	Of the 10 readings; 8 must be ≥ 7 mils and lowest individual reading must be ≥ 5 mils.

2	Machine direction (MD) and cross machine direction (XMD) average values should be on the basis of 5 test specimens each direction.

Yield elongation is calculated using a gauge length of 1.3 inches; Break elongation is calculated using a gauge length of 2.0 inches.

3	The yield stress used to calculate the applied load for the SP-NCTL test should be the mean value via MQC testing.

4	Other methods such as ASTM D 4218 or microwave methods are acceptable if an appropriate correlation can be established.

5	Carbon black dispersion for 10 different views: Nine in Categories 1 and 2 with one allowed in Category 3.

6	The condition of the test should be 20 hr. UV cycle at 75°C followed by 4 hr. condensation at 60°C.

7 	UV resistance is based on percent retained value regardless of the original HP-OIT value.

TEXTURED HDPE GEOMEMBRANE (METRIC UNITS)

Minimum Average Values

Property	Test Method	1.00 mm	1.50 mm	2.00 mm	2.50 mm

Thickness, microns	ASTM D 5994

minimum average		950	1,425	1,900	2,375

lowest individual of 8 of 10 readings		900	1,350	1,800	2,250

lowest individual of 10 readings		850	1,275	1,700	2,125

Asperity Height1, microns	ASTM D 7466	250	250	250	250

Sheet Density, g/cc	 ASTM D 1505/D 792	0.940	0.940	0.940	0.940

Tensile Properties2	ASTM D 6693

1. Yield Strength, kN/m	 	15	22	29	37

2. Break Strength, kN/m	 	11	16	21	26

3. Yield Elongation, %		12	12	12	12

4. Break Elongation, %		100	100	100	100

Tear Resistance, N	ASTM D 1004	125	187	249	311

Puncture Resistance, N	ASTM D 4833	267	400	534	667

Stress Crack Resistance3, hrs	ASTM D 5397 (App.)	300	300	300	300

Carbon Black Content4, %	ASTM D 1603	2.0 - 3.0	2.0 - 3.0	2.0 - 3.0	2.0 - 3.0

Carbon Black Dispersion	ASTM D 5596		                 --Note 5--

Oxidative Induction Time (OIT)

Standard OIT, minutes	ASTM D 3895	100	100	100	100

Oven Aging at 85°C	ASTM D 5721

High Pressure OIT - % retained after 90 days	ASTM D 5885		80	80	80	80

UV Resistance6	ASTM D 7238

High Pressure OIT7 - % retained after 1600 hrs	ASTM D 5885	50	50	50	50

Roll Dimensions

1. Width (meters):		7	7	7	7

2. Length (meters):		228.7	152.4	114.3	91.5

3. Area (square meters):		1,603	1,068	801	641

4. Gross weight (kilograms, approx):		1,588	1,588	1,574	1,574

1	Of the 10 readings; 8 must be ≥ 180 microns and lowest individual reading must be ≥ 130 microns.

2	Machine direction (MD) and cross machine direction (XMD) average values should be on the basis of 5 test specimens each direction.

Yield elongation is calculated using a gauge length of 33 mm; Break elongation is calculated using a gauge length of 50 mm.

3	The yield stress used to calculate the applied load for the SP-NCTL test should be the mean value via MQC testing.

4	Other methods such as ASTM D 4218 or microwave methods are acceptable if an appropriate correlation can be established.

5	Carbon black dispersion for 10 different views: Nine in Categories 1 and 2 with one allowed in Category 3.

6	The condition of the test should be 20 hr. UV cycle at 75°C followed by 4 hr. condensation at 60°C.

7 	UV resistance is based on percent retained value regardless of the original HP-OIT value.

SMOOTH LLDPE GEOMEMBRANE (ENGLISH UNITS)

Minimum Average Values

Property	Test Method	30 mil	40 mil	60 mil	80 mil

Thickness, mils	ASTM D 5199

minimum average		30	40	60	80

lowest individual reading		27	36	54	72

Sheet Density, g/cc (max.)	 ASTM D 1505/D 792	0.939	0.939	0.939	0.939

Tensile Properties1	ASTM D 6693

1. Break Strength, lb/in		114	152	228	304

2. Break Elongation, %		800	800	800	800

2% Modulus, lb/in2 (max.)	ASTM D 5323	60,000	60,000	60,000	60,000

Tear Resistance, lb	ASTM D 1004	16	22	33	44

Puncture Resistance, lb	ASTM D 4833	42	56	84	112

Axi-Symetric Break Strain, %	ASTM D 5617	30	30	30	30

Carbon Black Content2, %	ASTM D 1603	2.0 - 3.0	2.0 - 3.0	2.0 - 3.0	2.0 - 3.0

Carbon Black Dispersion	ASTM D 5596		                   --Note 3--

Oxidative Induction Time (OIT)

Standard OIT, minutes	ASTM D 3895	100	100	100	100

Oven Aging at 85°C	ASTM D 5721

High Pressure OIT - % retained after 90 days	                  ASTM D 5885		60	60	60	60

UV Resistance4	ASTM D 7238

High Pressure OIT5 - % retained after 1600 hrs	ASTM D 5885	35	35	35	35

Roll Dimensions

1. Width (feet):		23	23	23	23

2. Length (feet):		1,000	750	500	375

3. Area (square feet):		23,000	17,250	11,500	8,625

4. Gross weight (pounds, approx.):		3,435	3,435	3,435	3,435

1	Machine direction (MD) and cross machine direction (XMD) average values should be on the basis of 5 test specimens each direction. Break elongation is calculated using a gauge length of 2.0 inches.

2	Other methods such as ASTM D 4218 or microwave methods are acceptable if an appropriate correlation can be established.

3	Carbon black dispersion for 10 different views: Nine in Categories 1 and 2 with one allowed in Category 3.

4	The condition of the test should be 20 hr. UV cycle at 75°C followed by 4 hr. condensation at 60°C.

5	UV resistance is based on percent retained value regardless of the original HP-OIT value.

SMOOTH LLDPE GEOMEMBRANE (METRIC UNITS)

Minimum Average Values

Property	Test Method	0.75 mm	1.00 mm	1.50 mm	2.00 mm

Thickness, microns	ASTM D 5199

minimum average		750	1,000	1,500	2,000

lowest individual reading		675	900	1,350	1,800

Sheet Density, g/cc (max.)	 ASTM D 1505/D 792	0.939	0.939	0.939	0.939

Tensile Properties1	ASTM D 6693

1. Break Strength, kN/m		20	27	40	53

2. Break Elongation, %		800	800	800	800

2% Modulus, MPa (max.)	ASTM D 5323	414	414	414	414

Tear Resistance, N	ASTM D 1004	70	100	150	200

Puncture Resistance, N	ASTM D 4833	190	250	370	500

Axi-Symetric Break Strain, %	ASTM D 5617	30	30	30	30

Carbon Black Content2, %	ASTM D 1603	2.0 - 3.0	2.0 - 3.0	2.0 - 3.0	2.0 - 3.0

Carbon Black Dispersion	ASTM D 5596		                   --Note 3--

Oxidative Induction Time (OIT)

Standard OIT, minutes	ASTM D 3895	100	100	100	100

Oven Aging at 85°C	ASTM D 5721

High Pressure OIT - % retained after 90 days	                  ASTM D 5885		60	60	60	60

UV Resistance4	ASTM D 7238

High Pressure OIT5 - % retained after 1600 hrs	ASTM D 5885	35	35	35	35

Roll Dimensions

1. Width (meters):		7	7	7	7

2. Length (meters):		304.9	228.7	152.4	114.3

3. Area (square meters):		2,137	1,603	1,068	801

4. Gross weight (kilograms, approx.):		1,558	1,558	1,558	1,558

1	Machine direction (MD) and cross machine direction (XMD) average values should be on the basis of 5 test specimens each direction. Break elongation is calculated using a gauge length of 50 mm.

2	Other methods such as ASTM D 4218 or microwave methods are acceptable if an appropriate correlation can be established.

3	Carbon black dispersion for 10 different views: Nine in Categories 1 and 2 with one allowed in Category 3.

4	The condition of the test should be 20 hr. UV cycle at 75°C followed by 4 hr. condensation at 60°C.

5	UV resistance is based on percent retained value regardless of the original HP-OIT value.

TEXTURED LLDPE GEOMEMBRANE (ENGLISH UNITS)

Minimum Average Values

Property	Test Method	40 mil	60 mil	80 mil

Thickness, mils	ASTM D 5994

minimum average		38	57	76

lowest individual of 8 of 10 readings		36	54	72

lowest individual of 10 readings		34	51	68

Asperity Height1, mils	ASTM D 7466	10	10	10

Sheet Density, g/cc (max.)	 ASTM D 1505/D 792	0.939	0.939	0.939

Tensile Properties2	ASTM D 6693

1. Break Strength, lb/in		60	90	120

2. Break Elongation, %		250	250	250

2% Modulus, lb/in2 (max.)	ASTM D 5323	60,000	60,000	60,000

Tear Resistance, lb	ASTM D 1004	22	33	44

Puncture Resistance, lb	ASTM D 4833	44	66	88

Axi-Symetric Break Strain, %	ASTM D 5617	30	30	30

Carbon Black Content3, %	ASTM D 1603	2.0 - 3.0	2.0 - 3.0	2.0 - 3.0

Carbon Black Dispersion4	ASTM D 5596		--Note 4--

Oxidative Induction Time (OIT)

Standard OIT, minutes	ASTM D 3895	100	100	100

Oven Aging at 85°C	ASTM D 5721

High Pressure OIT - % retained after 90 days	                  ASTM D 5885		60		60	60

UV Resistance5	ASTM D 7238

High Pressure OIT6 - % retained after 1600 hrs	ASTM D 5885	35	35	35

Roll Dimensions

1. Width (feet):		23	23	23

2. Length (feet):		750	500	375

3. Area (square feet):		17,250	11,500	8,625

4. Gross weight (pounds, approx.):		3,465	3,465	3,435

1	Of the 10 readings; 8 must be ≥ 7 mils and lowest individual reading must be ≥ 5 mils.

2	Machine direction (MD) and cross machine direction (XMD) average values should be on the basis of 5 test specimens each direction. Break elongation is calculated using a gauge length of 2.0 inches.

3	Other methods such as ASTM D 4218 or microwave methods are acceptable if an appropriate correlation can be established.

4	Carbon black dispersion for 10 different views: Nine in Categories 1 and 2 with one allowed in Category 3.

5	The condition of the test should be 20 hr. UV cycle at 75°C followed by 4 hr. condensation at 60°C.

6 	UV resistance is based on percent retained value regardless of the original HP-OIT value.

TEXTURED LLDPE GEOMEMBRANE (METRIC UNITS)

Minimum Average Values

Property	Test Method	1.00 mm	1.50 mm	2.00 mm

Thickness, microns	ASTM D 5994

minimum average		950	1,425	1,900

lowest individual of 8 of 10 readings		900	1,350	1,800

lowest individual of 10 readings		850	1,275	1,700

Asperity Height1, microns	ASTM D 7466	250	250	250

Sheet Density, g/cc (max.)	 ASTM D 1505/D 792	0.939	0.939	0.939

Tensile Properties2	ASTM D 6693

1. Break Strength, kN/m		11	16	21

2. Break Elongation, %		250	250	250

2% Modulus, MPa (max.)	ASTM D 5323	414	414	414

Tear Resistance, N	ASTM D 1004	100	150	200

Puncture Resistance, N	ASTM D 4833	200	300	400

Axi-Symetric Break Strain, %	ASTM D 5617	30	30	30

Carbon Black Content3, %	ASTM D 1603	2.0 - 3.0	2.0 - 3.0	2.0 - 3.0

Carbon Black Dispersion4	ASTM D 5596		--Note 4--

Oxidative Induction Time (OIT)

Standard OIT, minutes	ASTM D 3895	100	100	100

Oven Aging at 85°C	ASTM D 5721

High Pressure OIT - % retained after 90 days	                  ASTM D 5885		60		60	60

UV Resistance5	ASTM D 7238

High Pressure OIT6 - % retained after 1600 hrs	ASTM D 5885	35	35	35

Roll Dimensions

1. Width (meters):		7	7	7

2. Length (meters):		228.7	152.4	114.3

3. Area (square meters):		1,603	1,068	801

4. Gross weight (kilograms, approx.):		1,572	1,572	1,558

1	Of the 10 readings; 8 must be ≥ 180 microns and lowest individual reading must be ≥ 130 microns.

2	Machine direction (MD) and cross machine direction (XMD) average values should be on the basis of 5 test specimens each direction. Break elongation is calculated using a gauge length of 2.0 inches.

3	Other methods such as ASTM D 4218 or microwave methods are acceptable if an appropriate correlation can be established.

4	Carbon black dispersion for 10 different views: Nine in Categories 1 and 2 with one allowed in Category 3.

5	The condition of the test should be 20 hr. UV cycle at 75°C followed by 4 hr. condensation at 60°C.

6 	UV resistance is based on percent retained value regardless of the original HP-OIT value.

2.4	Quality Control Specifications

2.4.1	Raw Materials

A.	Resin

All resins for use in geomembrane must pass a candidate pre-approval process before being eligible for use. Each incoming railcar shall be sampled by compartment with the following testing performed and compared to the manufacturer’s specifications:

1.	Density:  ASTM D 1505.

2.	Melt Index:  ASTM D 1238.

3.	Oxidative Induction Time (OIT):  ASTM D 3895.

B.	Additives

All incoming materials are to be tested and approved prior to use with the following testing performed and compared to the manufacturer’s specifications:

1.	Carbon Black Content:  ASTM D 1603.

2.	Oxidative Induction Time (OIT):  ASTM D 3895.

2.4.2	Finished Product: During Production

A.	Inspection

Performed on each roll during manufacturing.

1.	Appearance

Sheet surface appearance shall be monitored for flaws.

2.	Thickness

A full width sample shall be cut from the end of each roll for thickness measurement.

B.	Out-of-Spec. Material

Any roll not meeting the specification for any of the above inspections shall be separated from other rolls and placed on hold.

C.	Roll Identification

Four tags per roll shall be used.

1.	Inside the core.

2.	On the core plug.

3.	On the roll surface.

4.	On the production roll sample.

2.4.3	Manufacturer’s Quality Control & Quality Assurance Testing

A.	Sampling

Full width samples shall be taken as retains from the end of each roll to the manufacturer’s laboratory.

B.	Testing

The geomembrane quality control testing shall meet the following frequency requirements:

Property	Test Method	Testing Frequency (min.)

Thickness (smooth sheet)	ASTM D 5199	per roll

(textured sheet)	ASTM D 5994

Asperity Height (textured sheet only)	ASTM D 7466	every second roll

Alternate the measurement side for double-sided textured sheet.

Sheet Density	 ASTM D 1505/D 792	200,000 lb (90,000 kg)

Tensile Properties	ASTM D 6693	20,000 lb (9,000 kg)

1. Yield Strength (HDPE only)

2. Break Strength

3. Yield Elongation (HDPE only)

4. Break Elongation

2% Modulus (LLDPE only)	ASTM D 5323	per each formulation

Tear Resistance	ASTM D 1004	45,000 lb (20,000 kg)

Puncture Resistance	ASTM D 4833	45,000 lb (20,000 kg)

Axi-Symetric Break Strain (LLDPE only)	ASTM D 5617	per each formulation

Stress Crack Resistance (HDPE only)	ASTM D 5397 (App.)	per GRI GM10

Carbon Black Content	ASTM D 1603	20,000 lb (9,000 kg)

Carbon Black Dispersion	ASTM D 5596	45,000 lb (20,000 kg)

Oxidative Induction Time (OIT)

Standard OIT	ASTM D 3895	200,000 lb (90,000 kg)

Oven Aging at 85°C	ASTM D 5721

High Pressure OIT	ASTM D 5885	per each formulation

UV Resistance	ASTM D 7238

High Pressure OIT				                    ASTM D 5885			per each formulation

C.	Reporting

Results from the testing shall be reviewed by the quality control manager. Material that does not meet specifications shall be identified and placed on hold. The test data shall then be transferred to the product data file for roll certification.

3.	GEOMEMBRANE INSTALLATION

3.1	Materials Logistics

3.1.1	Transportation and On-site Storage

The geomembrane rolls shall be shipped by flatbed trailer to the job site. The geomembrane shall be stored so as to be protected from puncture, dirt, grease, moisture, and excessive heat. Damaged material shall be stored separately for repair or replacement. The rolls shall be stored on a prepared smooth surface (not wooden pallets) and should not be stacked more than two rolls high.

3.2	Earthwork

3.2.1	General

The owner or his representative (soil quality assurance inspector) shall inspect the subgrade preparation. Prior to liner installation the subgrade shall be compacted in accordance with the project specifications. Weak or compressible areas which cannot be satisfactorily compacted should be removed and replaced with properly compacted fill. All surfaces to be lined shall be smooth, free of all foreign and organic material, sharp objects, or debris of any kind. The subgrade shall provide a firm, unyielding foundation with no sharp changes or abrupt breaks in grade. Standing water or excessive moisture shall not be allowed.

The installer, on a daily basis, shall approve the surface on which the geomembrane will be installed. After the supporting soil surface has been approved, it shall be the installer’s responsibility to indicate to the inspector any changes to its condition that may require repair work.

3.2.2	Anchor Trench

The anchor trench shall be excavated to the line, grade, and width shown on the project construction drawings, prior to liner system placement. Slightly rounded corners shall be provided in the trench to avoid sharp bends in the geomembrane.

3.3	Method of Placement

The rolls shall be deployed using a spreader bar assembly attached to a loader bucket or by other methods approved by the project engineer.

The installer shall be responsible for the following:

1.	Equipment or tools shall not damage the geomembrane during handling, transportation , or deployment.

2.	Personnel working on the geomembrane shall not smoke or wear shoes that may damage the geomembrane.

3.	The method used to unroll the panels shall not cause scratches or crimps in the geomembrane and shall not damage the supporting soil.

4.	Adequate loading (e.g., sand bags or similar items that will not damage the geomembrane) shall be placed to prevent uplift by wind (in case of high winds, continuous loading is recommended along edges of panels to minimize risk of wind flow under the panels).

3.3.1	Weather Conditions

Geomembrane deployment shall proceed between ambient temperatures of 32° F and 104° F. Placement can proceed below 32° F only after it has been verified by the inspector that the material can be seamed according to the specification. Geomembrane placement shall not be done during any precipitation, in the presence of excessive moisture (e.g., fog, rain, dew) or in the presence of excessive winds, as determined by the installation supervisor.

3.4	Field Seaming

Approved seaming processes are fusion and extrusion welding. On side slopes, seams shall be oriented in the general direction of maximum slope, i.e., oriented down, not across the slope. In corners and odd-shaped geometric locations, the number of field seams shall be minimized.

No base T-seam shall be closer than 5 feet from the toe of the slope. Seams shall be aligned with the least possible number of wrinkles and “fishmouths”. If a fishmouth or wrinkle is found, it shall be relieved and cap-stripped.

3.4.1	Seam Overlap

Geomembrane panels must have a finished minimum overlap of 4 inches for fusion welding and 6 inches for extrusion welding.

Cleaning solvents may not be used unless the product is approved by the liner manufacturer.

3.4.2	Test Seams

Field test seams shall be conducted on the liner to verify that seaming conditions are satisfactory. Test seams shall be conducted at the beginning of each seaming period and at least once every 4 hours, for each seaming apparatus and personnel used that day.

All test seams shall be made in contact with the subgrade. Welding rod used for extrusion welding shall be manufactured from the same type of resin as the geomembrane. The test seam samples shall be 10 feet long for fusion welding and 3 feet long for extrusion welding with the seam centered lengthwise. Three specimens shall be cut from each end of the test seams by the inspector. The inspector shall use a tensiometer to test 3 specimens for shear and 3 specimens for peel. Each specimen shall be one inch wide with a grip separation of 4 inches plus the width of the seam. The seam shall be centered between the clamps.

3.4.3	Assessment of Seam Test Results

Seam testing shall be performed in accordance with ASTM D 6392 and meet the requirements of GRI GM 19.

3.4.4	Non-Destructive Seam Testing

The installer shall non-destructively test all field seams over their full length.

A.	Vacuum Box Testing

1.	Seam testing shall be performed in accordance with ASTM D 5641.

2.	All areas where animated soap bubbles appear shall be marked, repaired, and then retested.

B.	Air Pressure Testing (For Double Fusion Seams Only)

1.	Seam testing shall be performed in accordance with ASTM D5820.

2.	Energize the air pump to a pressure between 25 and 30 psi, allow 2 minutes for the injected air to come to equilibrium in the channel, and sustain pressure for approximately 5 minutes.

3.	If loss of pressure exceeds 4 psi, or pressure does not stabilize, locate faulty area, repair, and retest.

The following procedures shall apply to locations where seams cannot be non-destructively tested:

1.	If the seam is accessible to testing equipment prior to final installation, the seam shall be non-destructively tested prior to final installation.

2.	If the seam cannot be tested prior to final installation, the seam shall be spark tested according to the spark tester manufacturer’s procedures.

3.4.5	Destructive Seam Testing

Destructive seam testing should be minimized to preserve the integrity of the liner. The installer shall provide the inspector with one destructive test sample per project specifications (usually once per 500 feet of seam length) from a location specified by the inspector.

A.	Sampling Procedure

In order to obtain test results prior to completion of liner installation, samples shall be cut by the installer as the seaming progresses. The installer shall also record the date, location, and pass or fail description. All holes in the geomembrane resulting from obtaining the seam samples shall be immediately patched and vacuum tested.

B.	Size and Disposition of Samples

The samples shall be 12 inches wide by 36 inches long with the seam centered lengthwise. The sample shall be cut into three equal-length pieces, one to be given to the inspector, one to be given to the owner, and one to the installer.

C.	Field Laboratory Testing

Seam testing shall be performed in accordance with ASTM D 6392 and meet the requirements of GRI GM 19.

D.	Independent Laboratory Testing

The owner, at his discretion and expense, may send seam samples to a laboratory for testing. The test method and procedures to be used by the independent laboratory shall be the same as used in field testing.

E.	Procedures for Destructive Test Failure

The following procedures shall apply whenever a sample fails the field destructive test:

1.	The installer shall cap strip the seam between the failed location and any passed test locations.

2.	The installer can retrace the welding path to an intermediate location (usually 10 feet from the location of the failed test), and take a sample for an additional field test. If this test passes, then the seam shall be cap stripped between that location and the original failed location. If the test fails, then the process is repeated.

3.	Over the length of seam failure, the installer shall either cut out the old seam, reposition the panel and reseam, or add a cap strip.

3.4.6	Repairs

All seams and non-seam areas of the geomembrane shall be inspected by the inspector. The surface of the geomembrane shall be clean at the time of inspection.

A.	Evaluation

Each suspect location in seam and non-seam areas shall be non-destructively tested as appropriate in the presence of the inspector. Each location that fails the non-destructive testing shall be marked by the inspector and repaired accordingly.

B.	Repair Procedures

1.	Defective seams shall be cap stripped or replaced.

2.	Small holes shall be repaired by extrusion welding a bead of extrudate over the hole. If the hole is larger than 1/4 inch, it shall be patched.

3.	Tears shall be repaired by patching. If the tear is on a slope or an area susceptible to stress and has a sharp end it must be rounded prior to patching.

4.	Large cuts shall be repaired by patches.

5.		Patches shall be completed by extrusion welding. The weld area shall be ground no more than 10 minutes prior to welding. No more than 10% of the thickness shall be removed by grinding. Welding shall commence where the grinding started and must overlap the previous seam by at least 2 inches. Reseaming over an existing seam without regrinding shall not be permitted. The welding shall restart by grinding the existing seam and rewelding a new seam.

6.	Patches shall be round or oval in shape, made of the same geomembrane, and extend a minimum of 6 inches beyond the edge of defects.

C.	Verification of Repairs

Each repair shall be non-destructively tested. Repairs that pass the non-destructive test shall be taken as an indication of an adequate repair. Failed tests indicate that the repair shall be repeated and retested until passing test results are achieved.

The inspector shall keep daily documentation of all non-destructive and destructive testing. This documentation shall identify all seams that initially failed the test and include evidence that these seams were repaired and successfully retested.

3.5	Cover Material and Backfilling of Anchor Trench

The geomembrane shall be covered as soon as possible. The covering operation shall not damage the geomembrane. The cover soil material shall be free of foreign and organic material, sharp objects, or debris of any kind, which could potentially damage the geomembrane. No construction equipment or machinery that may damage the geomembrane shall operate directly on the geomembrane. The use of lightweight machinery (e.g., generator, etc.) with low ground pressure is allowed.

The anchor trench shall be backfilled by the earthwork contractor. Trench backfill material shall be placed and compacted in accordance with the project specifications.

Care shall be taken when backfilling the trenches to prevent any damage to the geomembrane. If damage occurs, it shall be repaired prior to backfilling.

3.6	Geomembrane Acceptance

The installer shall retain all ownership and responsibility for the geomembrane until accepted by the owner.

Final acceptance is when all of the following conditions are met:

1.	Installation is complete.

- Verification of the adequacy of all field seams and repairs, including associated testing, is complete.

END OF SECTION